[image: image1][image: image2.png]creating better environments




[image: image3.png][Rodbo

FLOORING SYSTEMS





To complete the clause, select the appropriate wording from below. Highlighted text can be ‘dragged and dropped’ to save typing.

M50 RUBBER/ PLASTICS/ CORK/ LINO/ CARPET TILING/ SHEETING
130 CARPET TILE: 
Tessera Format   A textured loop pile carpet tile. Manufactured from 80% solution dyed, 20% space dyed polyamide, on a modified bitumen polyester primary and secondary backing. Also available in SOFTbac®. Softbac® is an additional backing layer which also acts as an underlay and offers increased sound and thermal insulation and extends the guarantee period by 50% to 15 years. All colours of Format are available with the Tessera Direct guarantee, for more information please visit www.forbo-flooring.co.uk
Tile size: 50 x 50cm, other sizes are available for special orders. 

Pile weight: 525g/sm ± 10%

Thickness: 6.1mm ± 10%; With SOFTbac® + 3mm ± 10%.
Format is available in 18 colourways.

Tessera carpet tiles must be laid in accordance with best practice techniques as detailed in the Contract Flooring Association’s guidelines and BS5325.  Consult with Forbo technical literature for further details.

130 CARPET TILE:
Manufacturer: Forbo Flooring UK Ltd, P O Box 1, Kirkcaldy Fife, KY1 2SB. 

Tel: 0800 0282 162 Fax: 01772 646912; Tel

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk 

Product reference: Format
Type: Textured loop pile 
BS EN 1307 classification: Class 33
Level of use class: Heavy Contract
Size: 50 x 50cm
Colour/ pattern: As per finishes schedule
Method of Laying: Format can be installed Broadloom/Quarter Turn/Tessellated (delete as appropriate).

Adhesive: 542 Eurofix Tack Plus.

Accessories: Edging and cover strips, as clause 740.







PAGE  
1
[image: image3.png]Issue Date: September 2009

