[image: image1][image: image2.png]creating better environments




[image: image3.png][Rodbo

FLOORING SYSTEMS





Wet Room Solution Overview

This document provides an overview of the products and accessories that make up the Forbo Wet Room system, and guidance to be used when creating NBS specifications for the Forbo Wet Room System. If any further information is required please contact Forbo Flooring UK Ltd.
The Forbo wet room system comprises a choice vinyl floor coverings and a vinyl wall covering specifically designed for wet room applications in homes, hospitals, schools, offices and leisure facilities. This type of system provides no breeding ground for bugs and bacteria, such as MRSA, overcoming infection control concerns that may be associated with traditional tile & grout.


Onyx+ is a durable vinyl wall covering, especially suited for wet rooms, such as bathrooms and showers. Onyx must be heat welded to provide a smooth, hygienic surface that ensures no breeding ground for bugs and bacteria. Onyx sheet is 2000 mm wide x 0.92 mm thick and available in 17 colours.

Forbo Safestep Aqua, Surestep Laguna and Surestep Star Barefoot safety floor coverings have been designed for use in conjunction with the Onyx+ vinyl wall covering, which combine to ensure a completely watertight finish. Safestep Aqua and Surestep Laguna or Surestep Star Barefoot can be used alongside each other in different wet area zones if required e.g. Safestep Aqua in the wet shower zone and Surestep Laguna or Surestep Star Barefooot in the drying/changing area.

All three ranges can also be co-ordinated with Forbo’s other product ranges, including Surestep safety floors, Eternal sheet vinyl, Allura LVT, Flotex flocked flooring, Tessera & Westbond carpet tiles and Marmoleum.

The choice of floor covering, Safestep Aqua, Surestep Laguna or Surestep Barefoot will depend on the application. The following overview of each is intended to help in the selection process. For full product information view the product literature and technical specifications of visit use the following weblink;

www.forbo-flooring.co.uk/step
150 SHEETING: VINYL
Flooring roll: Heterogeneous PVC to BS EN ISO 10582 and BS EN 13845

Manufacturer: Forbo Flooring UK Ltd, High Holborn Road, Ripley, DE5 3NT

Tel: 0800 0282 162 Fax: 01772 646912 
Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk 
Product reference: Forbo Safestep Aqua . 
BS ISO 10874/ BS IS010852/BS EN13845 class: 34 / 43.

Safestep Aqua. A heterogeneous safety vinyl collection with a structured embossed surface offered in both Neutral and pastel colours. With slip resistant particles and PUR surface finish, Safestep Aqua combines durable slip resistance guaranteed for the product lifetime and ease of maintenance.

Safestep Aqua is designed for use in areas where high levels of barefoot wet slip resistance are required such as pool surrounds and shower areas and offers the following slip resistance performance properties:

· BS EN 13845: Class ESf (barefoot).
· Wet pendulum values   Slider 55 (barefoot applications): ≥36.
· Surface roughness: ≥20 µm.

· Ramp test (DIN 51130): R10.
· Barefoot ramp test (DIN 51097): Class C (highest classification).
Roll width: 2000 mm. Thickness: 2.0 mm. Thickness of wear layer: 0.7 mm.                          Colours/Patterns: 8 colours

Matching welding rods are available in all collection colours. 
Consult with Forbo technical literature for details.

Surestep Laguna. A heterogeneous safety vinyl collection with a fine structured surface offered in both Neutral and pastel colours. With slip resistant particles and PUR pearl surface finish, Surestep Laguna combines durable slip resistance guaranteed for the product lifetime and ease of maintenance.

Surestep Star Barefoot. A heterogeneous safety vinyl collection with a fine structured surface with slip resistant particles with decorative contrasting coloured decorative chips, and PUR pearl surface finish, Surestep Star Barefoot combines durable slip resistance guaranteed for the product lifetime and ease of maintenance.
Surestep Laguna and Surestep Star Barefoot are designed for use in areas where both shod (footwear) and barefoot wet slip resistance is required such as wet changing rooms and assisted bathrooms, and offers the following slip resistance performance:

· BS EN 13845: Classes ESb (shod) and ESf (barefoot).
· Wet pendulum values   Slider 96 (shod test) and slider 55 (barefoot applications): ≥36.
· Surface roughness: ≥20 µm.

· Ramp test (DIN 51130): R10.
· Barefoot ramp test (DIN 51097): Class B.
Roll width: 2000 mm. Thickness: 2.0 mm. Thickness of wear layer: 0.7 mm.                          Colours/Patterns: Surestep Laguna – 12 colours; Surestep Start Barefoot - 3 colours.

Matching welding rods are available in all collection colours. 
Consult with Forbo technical literature for details.

Surestep can also be specified in clause 155 (modified).                           
NBS Product Clauses – Floor coverings and skirtings
M50 SHEETING………..

Safestep Aqua. 
150 SHEETING: VINYL
Optional Fabricated underlay: [Select one from the list below if required]                                                                                                                         Forbo Corkment Underlay. 









     Forbo Vinylbase acoustic underlay 

BS ISO 10874/BS EN10852/BS EN13845 class: 34 / 43.

Width: 2000 mm.
Thickness: 2.0 mm.
Slip Resistance:

· BS EN 13845: Classes ESb (shod) and ESf (barefoot).

· Wet pendulum values   Slider 96 (shod test) and slider 55 (barefoot applications): ≥36.

· Surface roughness: ≥20 µm.

· Ramp test (DIN 51130): R10.

· Barefoot ramp test (DIN 51097): Class C (highest classification).

Colour/ pattern: 180092/180352/180232/180862/18048/180212/180592/180262
Adhesive (and primer if recommended by manufacturer):
Eurocol 540 Eurosafe Special – A superior acrylic dispersion solvent-free floor covering adhesive with a high initial grab.
Eurocol 640 Eurostar Special – A superior acrylic dispersion low VOC emission adhesive with a high initial grab.
Eurocol 140 Euromix PU – A polyurethane resin and hardener, water-resistant 2-component PU-adhesive.
Eurocol 233 Eurosol Contact – A synthetic rubber in solvent fast setting contact adhesive.
Seam welding: Hot welding with matching coloured rod.
Accessories: Skirtings, as clause 770.

Finishing: As clause 820 omitting polish finish.
Other requirements: Seek advice from Forbo for specific requirements for flooring.

Surestep Laguna. 
150 SHEETING: VINYL
Flooring roll: Heterogeneous PVC to BS EN ISO 10582 and BS EN 13845

Manufacturer: Forbo Flooring UK Ltd, High Holborn Road, Ripley, DE5 3NT

Tel: 0800 0282 162 Fax: 01772 646912 

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk 
Product reference: Forbo Surestep Laguna. 
BS ISO 10874/ BS IS010852/BS EN13845 class: 34 / 43.

Width: 2000 mm.
Thickness: 2.0 mm.
Slip Resistance:

· BS EN 13845: Classes ESb (shod) and ESf (barefoot).

· Wet pendulum values   Slider 96 (shod test) and slider 55 (barefoot applications): ≥36.

· Surface roughness: ≥20 µm.

· Ramp test (DIN 51130): R10.

· Barefoot ramp test (DIN 51097): Class B (highest classification).

Colour/ pattern: 181092/ 181262/ 181862/ 181072/ 181592/ 181692/ 181482/ 181912/ 181632/ 181912/ 181972/ 181982/ 181822/ 181802/ 181882

Adhesive (and primer if recommended by manufacturer):
Eurocol 540 Eurosafe Special – A superior acrylic dispersion solvent-free floor covering adhesive with a high initial grab.
Eurocol 640 Eurostar Special – A superior acrylic dispersion low VOC emission adhesive with a high initial grab.
Eurocol 140 Euromix PU – A polyurethane resin and hardener, water-resistant 2-component PU-adhesive.
Eurocol 233 Eurosol Contact – A synthetic rubber in solvent fast setting contact adhesive.
Seam welding: Hot welding with matching coloured rod.
Accessories: Skirtings, as clause 770.

Finishing: As clause 820 omitting polish finish.
Other requirements: Seek advice from Forbo for specific requirements for flooring.
770 Skirtings
Type: Self coved skirting: Cove former: Quantum Profiles reference QCF35 - 35mm radius tapered to architraves. Securely bond to base and background using contact adhesive. Corner coving profiles Quantum Internal Trimitre CCTM1 and external Floormitre CCFM2.
Top edge trim: Quantum Profiles QT200 – 2mm PVC diminishing strip. Securely bond to background using contact adhesive, with top edge straight and parallel with floor.

Turn flooring material up wall, securely bond to cove former and background using adhesive specified for fixing to base, and fit top edge trim. Accurately mitre at corners. All joints to be hot welded in accordance with the manufacturer’s instructions.

Height: 100mm

Surestep Star Barefoot  
150 SHEETING: VINYL
Flooring roll: Heterogeneous PVC to BS EN ISO 10582 and BS EN 13845

Manufacturer: Forbo Flooring UK Ltd, High Holborn Road, Ripley, DE5 3NT

Tel: 0800 0282 162 Fax: 01772 646912 

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk 
Product reference: Forbo Surestep Star Barefoot 
BS ISO 10874/ BS IS010852/BS EN13845 class: 34 / 43.

Width: 2000 mm.
Thickness: 2.0 mm.
Slip Resistance:

· BS EN 13845: Classes ESb (shod) and ESf (barefoot).

· Wet pendulum values   Slider 96 (shod test) and slider 55 (barefoot applications): ≥36.

· Surface roughness: ≥20 µm.

· Ramp test (DIN 51130): R10.

· Barefoot ramp test (DIN 51097): Class B (highest classification).

Colour/ pattern: 178082/ 178032/ 178922


Adhesive (and primer if recommended by manufacturer):
Eurocol 540 Eurosafe Special – A superior acrylic dispersion solvent-free floor covering adhesive with a high initial grab.
Eurocol 640 Eurostar Special – A superior acrylic dispersion low VOC emission adhesive with a high initial grab.
Eurocol 140 Euromix PU – A polyurethane resin and hardener, water-resistant 2-component PU-adhesive.
Eurocol 233 Eurosol Contact – A synthetic rubber in solvent fast setting contact adhesive.
Seam welding: Hot welding with matching coloured rod.
Accessories: Skirtings, as clause 770.

Finishing: As clause 820 omitting polish finish.
Other requirements: Seek advice from Forbo for specific requirements for flooring.

770 Skirtings
Type: Self coved skirting: Cove former: Quantum Profiles reference QCF35 - 35mm radius tapered to architraves. Securely bond to base and background using contact adhesive. Corner coving profiles Quantum Internal Trimitre CCTM1 and external Floormitre CCFM2.
Top edge trim: Quantum Profiles QT200 – 2mm PVC diminishing strip. Securely bond to background using contact adhesive, with top edge straight and parallel with floor.

Turn flooring material up wall, securely bond to cove former and background using adhesive specified for fixing to base, and fit top edge trim. Accurately mitre at corners. All joints to be hot welded in accordance with the manufacturer’s instructions.

Height: 100mm

NBS Specification data – Onyx+
K13 – 145 Proprietary Plastics Cladding
Flooring roll: Heterogeneous PVC wall covering to BS EN15102:2007+A1:2011
Fire Rating: EN13501-1 Class Bs2-d0


Manufacturer: Forbo Flooring UK Ltd, High Holborn Road, Ripley, DE5 3NT

Tel: 01773 744121 Fax: 01772 646912 

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk 
Product reference: Onyx+ vinyl wall covering
Identity code: Consult with Forbo Flooring for details.

Width: 2000 mm
Thickness: 0.92 mm
Length: 30m 

Colour/ pattern: 26500/ 26501/ 26504/ 26505/ 26507/ 26508/ 26511/ 26514/ 26517/ 26518/ 26520/ 26521/ 26524/ 26537/ 26547/ 26548
Adhesive (and primer if recommended by manufacturer): Contact Forbo Flooring for installation and adhesive recommendations
Seam welding: Seams should be hot seam welded using matching weld cable. Overlap seams between floor covering and wall covering should be cold welded – consult Forbo Flooring for recommended procedures and products.
Accessories: Cove former: Quantum Profiles reference QCF35 - 35mm radius to all internal corners. Corner Profile: Quantum Profiles reference EFA75 to all external corners. Securely bond to base and background using contact adhesive. 
Top edge trim: Quantum Profiles QT100 – 1mm PVC diminishing strip. Securely bond to background using contact adhesive, with top edge straight and parallel with floor.

Finishing: As per manufactures recommendations
Other requirements: Seek advice from Forbo Flooring Ltd for specific requirements for the installation of wall coverings in wet rooms.
PAGE  
1
[image: image3.png]Issue Date: January 2018

