[image: image1][image: image2.png]creating better environments




[image: image3.png][Rodbo

FLOORING SYSTEMS





To complete the clause, select the appropriate wording from below. Highlighted text can be ‘dragged and dropped’ to save typing.

M50 RUBBER/ PLASTICS/ CORK/ LINO/ CARPET TILING/ SHEETING
150 SHEETING: . . . . . .
Surestep Decibel: A range of heterogeneous safety vinyl floor coverings, with an acoustic foam backing and high-density calendared wear layer incorporating hard particles for enhanced slip resistance. 
Surestep Decibel meets the requirements of EN13845 for PVC floor coverings with particle based enhanced slip resistance and offers additional acoustic insulation with an excellent impact sound reduction of 17dB without concessions to the performance. Surestep Decibel is suitable for use in Class 34, very heavy commercial use, areas. 
Roll width: 2000 or 4000 mm.   Thickness: 3 mm.   Thickness of wear layer: 0.7 mm.
Colours/patterns:  4 x Surestep original Decibel: 4 x Surestep Material Decibel; 4 x Surestep Wood Decibel
Matching welding rods are available in all collection colours. 
Consult with Forbo technical literature for details.

150 SHEETING: VINYL

Fabricated underlay (delete where not required)                                                                                                                        Forbo QuickFit Subfloor System. – Optional.


Flooring roll:  Heterogeneous PVC to BS EN13845 and BS EN 651 (ISO 11638).

Manufacturer: Forbo Flooring UK Ltd, P O Box 1, Kirkcaldy Fife, KY1 2SB. 

Tel: 0800 0282 162 Fax: 01772 646912 

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk 

Product reference: Forbo Surestep Decibel. 
BS EN13845 / BS ISO 10874 class:  34 / 42
Width: 2000 / 4000mm [delete as appropriate]
Thickness: 3 mm.


Slip Resistance:

· BS EN 13845: Classes ESb (shod).

· Wet pendulum values   Slider 96: ≥36.

· Surface roughness: ≥20 µm.

· Ramp test (DIN 51130): R10.

Colour/ pattern: Select from the following colours: 
Surestep Original Decibel: 7172862/7171072/7172092/7171592
Surestep Material Decibel: 717122/717422/717482/717172

Surestep Wood Decibel: 718972/718962/718882/718802
Adhesive (and primer if recommended by manufacturer):
Eurocol 540 Eurosafe Special – A superior acrylic dispersion solvent-free floor covering adhesive with a high initial grab.
Eurocol 640 Eurostar Special – A superior acrylic dispersion low VOC emission adhesive with a high initial grab.
Eurocol 233 Eurosol Contact – A synthetic rubber in solvent fast setting contact adhesive.
Seam welding: Hot welding with matching coloured rod.
Accessories:
Edging and cover strips, as clause 740.
Stair nosing, as clause 750.
Skirtings, as clause 770.
Finishing: As clause 820 omitting polished finish.
Other requirements: Seek advice from Forbo for specific requirements for flooring.

770 Skirtings

Type: Self coved skirting

Cove former: Quantum Profile Systems reference QCF35 - 35mm radius tapered to architraves. Securely bond to base and background using contact adhesive. Accurately mitre at corners. 

Capping strip: Quantum Profile Systems UCS2 PVC capping strip. Where wall finish is ceramic tiles use Quantum Profiles QCT1.

Securely bond to background using contact adhesive, with top edge straight and parallel with floor.

Turn flooring material up wall, securely bond to cove former and background using adhesive specified for fixing to base, and ease top of material into edge trim. Accurately mitre at corners. All joints to be hot welded in accordance with the manufacturer’s instructions.

Height: [insert required height] mm

PAGE  
2
[image: image3.png]Issue Date: February 2018

