Wet Room Solution Overview

This document provides an overview of the products and accessories that make up the Forbo Wet Room system, and guidance to be used when creating NBS specifications for the Forbo Wet Room System. If any further information is required please contact Forbo Flooring UK Ltd.

The Forbo wet room system comprises a choice vinyl floor coverings and  a vinyl wall covering specifically designed for wet room applications in homes, hospitals, schools, offices and leisure facilities. This type of system provides no breeding ground for bugs and bacteria, such as MRSA, overcoming infection control concerns that may be associated with traditional tile & grout.

Onyx FR is a durable vinyl wall covering, especially suited for wet rooms, such as bathrooms and showers. Onyx must be heat welded to provide a smooth, hygienic surface that ensures no breeding ground for bugs and bacteria. Onyx sheet is 2000 mm wide x 0.92 mm thick and available in 20 colours.

Forbo Safestep Aqua and Surestep Laguna safety floor coverings have been designed for use in conjunction with the Onyx FR vinyl wall covering, which combine to ensure a completely watertight finish. Safestep Aqua and Surestep Laguna can be used alongside each other in different wet area zones if required e.g. Safestep Aqua in the wet shower zone and Surestep Laguna in the drying/changing area.

Both ranges can also be co-ordinated with Forbo’s other product ranges, including Surestep safety floors, Eternal sheet vinyl, Allura LVT, Flotex flocked flooring, Tessera & Westbond carpet tiles and Marmoleum.

The choice of floor covering, either Safestep Aqua or Surestep Laguna will depend on the application. The following overview of each is intended to help in the selection process. For full product information view the product literature and technical specifications of visit use the following weblinks;

Safestep Aqua. A heterogeneous safety vinyl collection with a structured embossed surface offered in both Neutral and pastel colours. With slip resistant particles and PUR surface finish, Safestep Aqua combines durable slip resistance guaranteed for the product lifetime and ease of maintenance.

Safestep Aqua is designed for use in areas where high levels of barefoot wet slip resistance are required such as pool surrounds and shower areas and offers the following slip resistance performance properties:

- BS EN 13845: Class ESf (barefoot).

- Wet pendulum values   Slider 55 (barefoot applications): ≥36.

- Surface roughness: ≥20 µm.

- Ramp test (DIN 51130): R10.

- Barefoot ramp test (DIN 51097): Class C (highest classification).

Surestep Laguna. A heterogeneous safety vinyl collection with a fine structured surface offered in both Neutral and pastel colours. With slip resistant particles and PUR pearl surface finish, Surestep Laguna combines durable slip resistance guaranteed for the product lifetime and ease of maintenance.

Surestep Laguna is designed for use in areas where both shod (footwear) and barefoot wet slip resistance is required such as wet changing rooms and assisted bathrooms, and offers the following slip resistance performance:

- BS EN 13845: Classes ESb (shod) and ESf (barefoot).

- Wet pendulum values   Slider 96 (shod test) and slider 55 (barefoot applications): ≥36.

- Surface roughness: ≥20 µm.

- Ramp test (DIN 51130): R10.

- Barefoot ramp test (DIN 51097): Class B.

Safestep Aqua and Surestep Laguna are 2000 mm and 2.0 mm overall thickness with a wear layer thickness of 0.7mm. Each range is offered in 12 common colours.

Matching weld rods are available for both Step and & Onyx FR.  Consult Forbo Flooring for details, samples and colour availability.

NBS Product Clauses – Floor coverings and skirtings

M50 SHEETING………..

Safestep Aqua.

150 SHEETING: VINYL

Optional Fabricated underlay: [Select one from the list below if required]                                                                                                                                    Forbo Corkment Underlay. 										     Forbo Vinylbase acoustic underlay

Flooring roll: Heterogeneous PVC to BS EN ISO 10582 and BS EN 13845

Manufacturer: Forbo Flooring UK Ltd, P O Box 1, Kirkcaldy Fife, KY1 2SB.

Tel: 0800 0282 162 Fax: 01772 646912

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk

Product reference: Forbo Safestep Aqua.

BS ISO 10874/BS EN10852/BS EN13845 class: 34 / 43.

Width: 2000 mm.
Thickness: 2.0 mm.

Slip Resistance:

- BS EN 13845: Classes ESb (shod) and ESf (barefoot).

- Wet pendulum values   Slider 96 (shod test) and slider 55 (barefoot applications): ≥36.

- Surface roughness: ≥20 µm.

- Ramp test (DIN 51130): R10.

- Barefoot ramp test (DIN 51097): Class C (highest classification).

Colour/ pattern: 180012 / 180262 / 180152 / 180292 / 180202 / 180232 / 180352 / 180052 / 180182 / 180322 / 180092 / 180122

Adhesive (and primer if recommended by manufacturer):
Eurocol 540 Eurosafe Special – A superior acrylic dispersion solvent-free floor covering adhesive with a high initial grab.
Eurocol 640 Eurostar Special – A superior acrylic dispersion low VOC emission adhesive with a high initial grab.
Eurocol 140 Euromix PU – A polyurethane resin and hardener, water-resistant 2-component PU-adhesive.
Eurocol 233 Eurosol Contact – A synthetic rubber in solvent fast setting contact adhesive.

Seam welding: Hot welding with matching coloured rod.

Accessories: Skirtings, as clause 770.

Finishing: As clause 820 omitting polish finish.

Other requirements: Seek advice from Forbo for specific requirements for flooring.

Surestep Laguna.

150 SHEETING: VINYL

Flooring roll: Heterogeneous PVC to BS EN ISO 10582 and BS EN 13845

Manufacturer: Forbo Flooring UK Ltd, P O Box 1, Kirkcaldy Fife, KY1 2SB.

Tel: 0800 0282 162 Fax: 01772 646912

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk

Product reference: Forbo Surestep Laguna.

BS ISO 10874/ BS IS010852/BS EN13845 class: 34 / 43.

Width: 2000 mm.
Thickness: 2.0 mm.

Slip Resistance:

- BS EN 13845: Classes ESb (shod) and ESf (barefoot).

- Wet pendulum values   Slider 96 (shod test) and slider 55 (barefoot applications): ≥36.

- Surface roughness: ≥20 µm.

- Ramp test (DIN 51130): R10.

- Barefoot ramp test (DIN 51097): Class C (highest classification).

Colour/ pattern: 181012 / 181262 / 181152 / 181292 / 181202 / 181232 / 181352 / 181052 / 181182 / 181322 / 181092 / 181122

Adhesive (and primer if recommended by manufacturer):
Eurocol 540 Eurosafe Special – A superior acrylic dispersion solvent-free floor covering adhesive with a high initial grab.
Eurocol 640 Eurostar Special – A superior acrylic dispersion low VOC emission adhesive with a high initial grab.
Eurocol 140 Euromix PU – A polyurethane resin and hardener, water-resistant 2-component PU-adhesive.
Eurocol 233 Eurosol Contact – A synthetic rubber in solvent fast setting contact adhesive.

Seam welding: Hot welding with matching coloured rod.

Accessories: Skirtings, as clause 770.

Finishing: As clause 820 omitting polish finish.

Other requirements: Seek advice from Forbo for specific requirements for flooring.

770 Skirtings

Type: Self coved skirting: Cove former: Quantum Profiles reference QCF35 - 35mm radius tapered to architraves. Securely bond to base and background using contact adhesive. Corner coving profiles Quantum Internal Trimitre CCTM1 and external Floormitre CCFM2.

Top edge trim: Quantum Profiles QT200 – 2mm PVC diminishing strip. Securely bond to background using contact adhesive, with top edge straight and parallel with floor.

Turn flooring material up wall, securely bond to cove former and background using adhesive specified for fixing to base, and fit top edge trim. Accurately mitre at corners. All joints to be hot welded in accordance with the manufacturer’s instructions.

Height: 100mm

NBS Specification data - Onyx FR

Flooring roll: Heterogeneous PVC wall covering to BS EN15102:2007+A1:2011

Fire Rating: EN13501-1 Class B-s2D0

Manufacturer: Forbo Flooring UK Ltd, High Holborn Road, Ripley, DE5 3NT

Tel: 01773 744121 Fax: 01772 646912

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk

Product reference: Onyx FR vinyl wall covering

Identity code: Consult with Forbo Flooring for details.

Width: 2000 mm
Thickness: 0.92 mm

Length: 30m

Colour/ pattern: [select from] 23537 /23539 / 23547 / 23546 / 23542 / 23543 / 23544 / 23545 / 23532 / 23550/ 23549 / 23548 / 23541 / 23557 / 23551 /23553 / 23552 / 23554 / 23556 / 23555

Adhesive (and primer if recommended by manufacturer): Contact Forbo Flooring for installation and adhesive recommendations

Seam welding: Seams should be hot seam welded using matching weld cable. Overlap seams between floor covering and wall covering be cold welded – consult Forbo Flooring for recommended procedures and products.

Accessories: Cove former: Quantum Profiles reference QCF35 - 35mm radius to all internal corners. Corner Profile: Quantum Profiles reference EFA75 to all external corners. Securely bond to base and background using contact adhesive.

Top edge trim: Quantum Profiles QT100 – 1mm PVC diminishing strip. Securely bond to background using contact adhesive, with top edge straight and parallel with floor.

Finishing: As per manufactures recommendations

Other requirements: Seek advice from Forbo Flooring Ltd for specific requirements for the installation of wall coverings in wet rooms.