To complete the clause, select the appropriate wording from below. Highlighted text can be ‘dragged and dropped’ to save typing.

M50 RUBBER/ PLASTICS/ CORK/ LINO/ CARPET TILING/ SHEETING

130 CARPET TILE:

Tessera Alignment   A cut and loop pile carpet tile. Manufactured from 100% solution dyed Invista Antron® Lumena polyamide, on a modified bitumen polyester primary and secondary backing. Also available in SOFTbac®. Softbac® is an additional backing layer which also acts as an underlay and offers increased sound and thermal insulation and extends the guarantee period by 50% to 15 years.

Tile size: 50 x 50cm, other sizes are available for special orders.

Pile weight (after shearing): 700g/sm ± 10%

Thickness: 6.2 mm ± 10%; With SOFTbac® + 3mm ± 10%.

Alignment is available in 24 colourways

Tessera carpet tiles must be laid in accordance with best practice techniques as detailed in the Contract Flooring Association’s guidelines and BS5325.  Consult with Forbo technical literature for further details.

130 CARPET TILE:

Manufacturer: Forbo Flooring UK Ltd, P O Box 1, Kirkcaldy Fife, KY1 2SB.

Tel: 0800 0282 162 Fax: 01772 646912

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk

Product reference: Alignment

Type: Cut and loop pile

BS EN 1307 classification: Class 33

Level of use class: Heavy Contract

Size: 50 x 50cm

Colour/ pattern: As per finishes schedule

Method of Laying: Alignment can be installed Monolithic/Quarter Turn/Tessellated (delete as appropriate).

Adhesive: 542 Eurofix Tack Plus.

Accessories: Edging and cover strips, as clause 740.