To complete the clause, select the appropriate wording from below. Highlighted text can be ‘dragged and dropped’ to save typing.

M50 RUBBER/ PLASTICS/ CORK/ LINO/ CARPET TILING/ SHEETING

130 CARPET TILE:

Tessera Create Space 1:   A tufted low level loop carpet tile. Manufactured from 100% regenerated ECONYL solution dyed polyamide 6, on a modified bitumen polyester primary and secondary backing. Also available in SOFTbac®. Softbac® is an additional backing layer which also acts as an underlay and offers increased sound and thermal insulation and extends the guarantee period by 50% to 15 years. Create Space 1 carpet tiles contain 75% recycled content by weight.

Tile size: 50 x 50cm, other sizes are available for special orders.

Pile weight: 500g/sm ± 10%

Thickness: 5.5mm ± 10%; With SOFTbac® + 3mm ± 10%.

Create Space 1 is available in 18 colourways.

Tessera carpet tiles must be laid in accordance with best practice techniques as detailed in the Contract Flooring Association’s guidelines and BS5325.  Consult with Forbo technical literature for further details.

130 CARPET TILE:

Manufacturer: Forbo Flooring UK Ltd, P O Box 1, Kirkcaldy Fife, KY1 2SB.

Tel: 0800 0282 162 Fax: 01772 646912; Tel 01592 643777 Fax: 01592 643999

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk

Product reference: Create Space 1

Type: Tufted low level loop carpet tile

BS EN 1307 classification: Class 33

Level of use class: Heavy Contract

Size: 50 x 50cm

Colour/ pattern: 1818 pearl | 1804 opal | 1819 jasper | 1813 nickel | 1822 sunstone | 1801 feldspar | 1807 tawny | 1821 citrine | 1824 kyanite | 1825 spinel | 1815 hematite | 1816 lithium | 1823 jadeite | 1827 lazulite | 1828 garnet | 1800 ebonite | 1820 agate | serpentine

Method of Laying: Monolithic/Quarter Turn/Tessellated (delete as appropriate).

Adhesive:  542 Eurofix Tack Plus.

Accessories: Edging and cover strips, as clause 740.