To complete the clause, select the appropriate wording from below.  Highlighted text can be ‘dragged and dropped’ to save typing.

M50 RUBBER / PLASTICS / CORK / LINO / CARPET TILING / SHEETING

M50 SHEETING……….

Sarlon® Oak and Oak Modern XL 15dB. Part of the Sarlon 15dB collection of heterogeneous project vinyl floor coverings with an acoustic performance of 15dB.  Its 0.7mm pure PVC wear layer provided with a PUR lacquer is outstandingly scratch and stain resistant.  Its unique construction delivers exceptional residual indentation with typical values of 0.05mm for easier movement of rolling loads and indoor wheeled traffic.

Roll width:  2000mm. Thickness:  2.6mm.  Thickness of wear layer:  0.7mm

Colours: Resin: 6 standard colourways

Matching welding rods are available in all collection colours

Consult with Forbo technical literature for details.

150 SHEETING: VINYL

Fabricated underlay: 
Forbo QuickFit Subfloor System – Optional – select only if required.

Flooring roll: Heterogeneous PVC to BS EN 651; ISO11638.

Manufacturer: Forbo Flooring UK Ltd, P O Box 1, Kirkcaldy Fife, KY1 2SB.

Tel: 0800 0282 162 Fax: 01772 646912

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk

Product reference: Forbo Sarlon Oak & Oak Modern 15dB

BS EN ISO 10874 class: 34 / 42
Width: 2000 mm
Thickness: 2.6 mm

Colour / pattern: [select from] 428422/428420/428430/428494/428483/428413

Adhesive (and primer if recommended by manufacturer):
Eurocol 540 Eurosafe Special – A superior acrylic dispersion solvent-free floor covering adhesive with a high initial grab - Specify for general purpose use.
Eurocol 640 Eurostar Special – A superior acrylic dispersion low VOC emission adhesive with a high initial grab – specify where BREEAM section HEA9 credits are required.

Eurocol 140 Euromix PU – A polyurethane resin and hardener, water-resistant 2-component PU-adhesive. – Specify where extremes of temperature or very heavy rolling loads are expected.

Seam welding: Hot welding with matching coloured rod.

Accessories:
Edging and cover strips, as clause 740.
Stair nosing, as clause 750.
Skirtings, as clause 770.

Finishing: As clause 820 omitting polish finish

Other requirements:  Seek advice from Forbo for specific requirements for flooring

770 Skirtings

Type: Self coved skirting

Cove former: Quantum Profile Systems reference QCF35 - 35mm radius tapered to architraves. Securely bond to base and background using contact adhesive. Accurately mitre at corners.

Capping strip: Quantum Profile Systems UCS2 PVC capping strip.

Securely bond to background using contact adhesive, with top edge straight and parallel with floor.

Turn flooring material up wall, securely bond to cove former and background using adhesive specified for fixing to base, and ease top of material into edge trim. Accurately mitre at corners. All joints to be hot welded in accordance with the manufacturer’s instructions.

Height: [insert required height] mm

460 SMOOTHING/LEVELLING UNDERLAYMENT COMPOUND

Forbo Flooring in association with Forbo Bonding Systems (Forbo Eurocol) manufacture a range of smoothing underlayment compounds.

Forbo Eurocol 902 Europlan Latex Premium
Forbo Eurocol 920 Europlan Alphy

Forbo Eurocol 902 Europlan Latex Premium
A cement based powder/latex mix smoothing compound. 902 Europlan Latex Premium can be used to prepare and smooth uneven internal subfloors such as power floated concrete, tamped or pan floated concrete, sand cement screeds, stone, flooring grade asphalt (min. 3mm and max. 6mm), plywood, non-flexing steel decks (mezzanine decks), thin, firmly bonded adhesive residues (min.3 mm), surface DPM’s, terrazzo granolithic, porcelain and ceramic tiles. For use in domestic, light commercial and industrial environments as a smoothing underlayment, prior to the application of resilient type floor finishes.

Although 902 Europlan Latex Premium can be used as a self-priming system, both porous and nonporous substrates are best primed, as this will help to increase inter bond adhesion and reduce the possibility of debonding issues occurring. When deemed a requirement, prime the base with 044 Europrimer Multi. See clause M50/10 and 20 ‘Preparation’ for details.

Consult Forbo Eurocol technical literature for details.

Type: Latex/Powder mix

Manufacturer: Forbo Flooring UK Ltd, P O Box 1, Kirkcaldy Fife, KY1 2SB.

Tel: 0800 0282 162 Fax: 01772 646912

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk

Product reference: Forbo Eurocol 902 Europlan Latex Premium

Application: Trowel or toothed smoothing trowel applied – minimum thickness 3mm. Protect fresh layers against draughts and direct sunlight.
When applying to an underfloor heated subfloor, the heating is to be turned off 24 hours before application and heat is not to be applied for at least 24 hours after application, in steps of 5°C per day.

Forbo Eurocol 920 Europlan Alphy
A self-smoothing, tension-free hardening levelling compound particularly suitable for anhydrite subfloors and designed for levelling in layers between 0.5 and 30mm thickness.
Smooth and impervious subfloors (ceramic, granolithic, terrazzo), asphalt and bituminous floors to be primed with 044 Europrimer Multi. Highly absorbent subfloors to be primed with 044 Europrimer Multi. See clause M50/10 and 20 ‘Preparation’ for details.
Consult Forbo Eurocol technical literature for details.

Type: Water/powder mix

Manufacturer: Forbo Flooring UK Ltd, P O Box 1, Kirkcaldy Fife, KY1 2SB.

Tel: 0800 0282 162 Fax: 01772 646912

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk

Product reference: Forbo Eurocol 920 Europlan Alphy

Application: Trowel or toothed smoothing trowel. Protect fresh layers against draughts and direct sunlight. When applying to an underfloor heated subfloor, the heating is to be turned off 24 hours before application and heat is not to be applied for at least 24 hours after application, in steps of 5°C per day.