To complete the clause, select the appropriate wording from below. Highlighted text can be ‘dragged and dropped’ to save typing.

M50 RUBBER/ PLASTICS/ CORK/ LINO/ CARPET TILING/ SHEETING

150 SHEETING: LINOLEUM

Marmoleum® acoustic. Part of the Marmoleum Marbled collection, Marmoleum Acoustic is a twin-layered acoustic linoleum designed to achieve 14 dB impact sound reduction (ISO 717-2). It is composed of a 2 mm Corkment under layer plus 2 mm of Marmoleum, which is calendared on the Corkment. Using Marmoleum acoustic saves on both installation and adhesive costs, because the product can be installed in one operation, avoiding the need to first install Corkment and then Marmoleum.

Roll width: 2000 mm. Thickness: 4.0 mm. Colours/ patterns: 6 standard colourways.
Matching welding rods are available in all collection colours.
Consult with Forbo technical literature for details.

Flooring roll: Linoleum to BS EN 687.
Manufacturer: Forbo Flooring, PO Box 1, Kirkcaldy, Fife KY1 2SB Tel: 01592 643777 Fax: 01592 643999 E-mail: info.uk@forbo.com Web: www.forbo-flooring.co.uk  
Product reference: Forbo Marmoleum® acoustic.
BS EN 685 class: 23 / 33 / 41.
Width: 2000 mm.
Thickness: 4.0 mm.
Colour/ pattern: As finishes schedule

Adhesive (and primer if recommended by manufacturer):
Eurocol 414/696 Euroflex Lino Plus – A synthetic resin dispersion adhesive with a high initial grab.
Eurocol 614 Eurostar Lino Plus – A superior acrylic dispersion very low VOC-emission adhesive with a high initial grab.
Eurocol 233 Eurosol Contact – A synthetic rubber in solvent fast setting contact adhesive.

Seam welding: Hot welding with matching coloured rod.

Accessories:
Edging and cover strips, as clause 740.
Stair nosing, as clause 750.
Skirtings, as clause 770.

Finishing: As clause 820 omitting polish finish.

Other requirements: 
Seek advice from Forbo for specific requirements for flooring.