To complete the clause, select the appropriate wording from below. Highlighted text can be ‘dragged and dropped’ to save typing.

M50 RUBBER/ PLASTICS/ CORK/ LINO/ CARPET TILING/ SHEETING

M50 SHEETING………..

Safestep Aqua. A heterogeneous safety vinyl collection with a structured embossed surface offered in both Neutral and pastel colours. With slip resistant particles and PUR surface finish, Safestep Aqua combines durable slip resistance guaranteed for the product lifetime and ease of maintenance.

Safestep Aqua is designed for use in areas where high levels of barefoot wet slip resistance are required such as pool surrounds and shower areas and offers the following slip resistance performance properties:

- BS EN 13845: Class ESf (barefoot).

- Wet pendulum values   Slider 55 (barefoot applications): ≥36.

- Surface roughness: ≥20 µm.

- Ramp test (DIN 51130): R10.

- Barefoot ramp test (DIN 51097): Class C (highest classification).

Roll width: 2000 mm. Thickness: 2.0 mm. Thickness of wear layer: 0.7 mm.                                     Colours/Patterns: 12 colours.

Matching welding rods are available in all collection colours. 
Consult with Forbo technical literature for details.

Surestep can also be specified in clause 155 (modified).

150 SHEETING: VINYL

Optional Fabricated underlay: [Select one from the list below if required]                                                                                                                                    Forbo Corkment Underlay.	     									       Forbo Vinylbase acoustic underlay

Flooring roll: Heterogeneous PVC to BS EN ISO 10582 and BS EN 13845

Manufacturer: Forbo Flooring UK Ltd, P O Box 1, Kirkcaldy Fife, KY1 2SB.

Tel: 0800 0282 162 Fax: 01772 646912

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk

Product reference: Forbo Safestep Aqua.

BS ISO 10874/BS EN10852/BS EN13845 class: 34 / 43.

Width: 2000 mm.
Thickness: 2.0 mm.

Slip Resistance:

- BS EN 13845: Class ESf (barefoot).

- Wet pendulum values   Slider 55 (barefoot applications): ≥36.

- Surface roughness: ≥20 µm.

- Ramp test (DIN 51130): R10.

- Barefoot ramp test (DIN 51097): Class C (highest classification).

Colour/ pattern: 180012 / 180262 / 180152 / 180292 / 180202 / 180232 / 180352 / 180052 / 180182 / 180322 / 180092 / 180122

Adhesive (and primer if recommended by manufacturer):
Eurocol 540 Eurosafe Special – A superior acrylic dispersion solvent-free floor covering adhesive with a high initial grab.
Eurocol 640 Eurostar Special – A superior acrylic dispersion low VOC emission adhesive with a high initial grab.
Eurocol 140 Euromix PU – A polyurethane resin and hardener, water-resistant 2-component PU-adhesive.
Eurocol 233 Eurosol Contact – A synthetic rubber in solvent fast setting contact adhesive.

Seam welding: Hot welding with matching coloured rod.

Accessories:
Edging and cover strips, as clause 740.
Stair nosing, as clause 750.
Skirtings, as clause 770.

Finishing: As clause 820 omitting polish finish.

Other requirements: Seek advice from Forbo for specific requirements for flooring.

770 Skirtings

Type: Self coved skirting

Cove former: Quantum Profiles reference QCF35 - 35mm radius tapered to architraves. Securely bond to base and background using contact adhesive. Accurately mitre at corners or, when the floor covering used in conjunction with Forb Onyx wall covering, use Quantum Internal Trimitre CCTM1 and External Floormitre CCFM2.

Top edge trim: Quantum Profiles UCS2 PVC capping strip or, when the floor covering used in conjunction with Forbo Onyx wall covering, use Quantum QT200 – 2mm PVC diminishing strip.

Securely bond to background using contact adhesive, with top edge straight and parallel with floor.

Turn flooring material up wall, securely bond to cove former and background using adhesive specified for fixing to base, and ease top of material into edge trim. Accurately mitre at corners. All joints to be hot welded in accordance with the manufacturer’s instructions.

Height: 100mm