To complete the clause, select the appropriate wording from below. Highlighted text can be ‘dragged and dropped’ to save typing.

M50 RUBBER/ PLASTICS/ CORK/ LINO/ CARPET TILING/ SHEETING

M50 SHEETING………..

Surestep Stone. A heterogeneous safety vinyl collection combining decorative stone and concrete designs with slip resistant particles and PUR pearl surface finish. Surestep Stone combines durable slip resistance guaranteed for the product lifetime and ease of maintenance required in general traffic areas where additional slip resistance properties are required.

Surestep Stone complies with BS EN 13845 Class ESb (shod), and offers wet pendulum values of >36 and a surface roughness of ≥ 20 microns. DIN51130 (Ramp test) - R10.

Surestep can also be specified in clause 155 (modified).

Roll width: 2000 mm. Thickness: 2.0 mm. Thickness of wear layer: 0.7 mm.                          Colours/Patterns: 8 colours.

Matching welding rods are available in all collection colours. 
Consult with Forbo technical literature for details.

150 SHEETING: VINYL

Fabricated underlay:                                                                                                                                       Forbo Corkment Underlay. – Optional.
Forbo QuickFit Subfloor System. – Optional.
Forbo Sarlibase T.E. Underlay. – Optional                                                                                                    Forbo Vinylbase acoustic underlay - Optional

Flooring roll: Heterogeneous PVC to BS EN ISO 10582 and BS EN 13845
Manufacturer: Forbo Flooring UK Ltd, P O Box 1, Kirkcaldy Fife, KY1 2SB.

Tel: 0800 0282 162 Fax: 01772 646912

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk

Product reference: Forbo Surestep Stone.

BS EN685/BS ISO 10874 class: 34 / 43.
Width: 2000 mm.
Thickness: 2.0 mm.

Pendulum test value (wet): ≥36

Surface Roughness: ≥20
Colour/ pattern: As per finishes Schedule
Adhesive (and primer if recommended by manufacturer):
Eurocol 540 Eurosafe Special – A superior acrylic dispersion solvent-free floor covering adhesive with a high initial grab.
Eurocol 640 Eurostar Special – A superior acrylic dispersion low VOC emission adhesive with a high initial grab.
Eurocol 140 Euromix PU – A polyurethane resin and hardener, water-resistant 2-component PU-adhesive.
Eurocol 233 Eurosol Contact – A synthetic rubber in solvent fast setting contact adhesive.

Seam welding: Hot welding with matching coloured rod.

Accessories:
Edging and cover strips, as clause 740.
Stair nosing, as clause 750.
Skirtings, as clause 770.

Finishing: As clause 820 omitting polish finish.

Other requirements: Seek advice from Forbo for specific requirements for flooring.

770 Skirtings

Type: Self coved skirting

Cove former: 38mm radius/20mm radius {delet as appropriate] tapered to architraves. Securely bond to base and background using contact adhesive. Accurately mitre at corners.

Top edge trim: Captile TC48 – supply only – to be fitted by others where wall finish is PVC Cladding or ceramic tiles. HCS48 PVC capping strip to all other areas. Securely bond to background using contact adhesive, with top edge straight and parallel with floor.

Turn flooring material up wall, securely bond to cove former and background using adhesive specified for fixing to base, and ease top of material into edge trim. Accurately mitre at corners. All joints to be hot welded in accordance with the manufacturer’s instructions.

Height: 100mm