To complete the clause, select the appropriate wording from below. Highlighted text can be ‘dragged and dropped’ to save typing.

M50 RUBBER/ PLASTICS/ CORK/ LINO/ CARPET TILING/ SHEETING

150 SHEETING: . . . . . .

Sphera EC

Sphera EC is Forbo’s homogeneous vinyl collection with conductive properties in sheet format.

The collection is specifically designed to control static discharges and particles in the most sensitive environments, such as pharmaceutical, life sciences and healthcare facilities. Innovative product development and carefully controlled production processes ensure a solution with permanent conductive properties, which comply with all ESD standards:

Produced using permanently conductive materials, Sphera EC sheet vinyl is guaranteed to retain its optimal performance throughout the product’s lifetime, regardless of the conditions of the environment, such as humidity levels.

It is produced using green energy in a zero-waste environment, ensuring efficient and sustainable manufacturing and the low emissions and phthalate free manufacturing ensures contribution to a healthy indoor environment

The conductive backing applied as part of the production process means that there is no need for conductive adhesive underneath the full sheet, only to affix the copper strip for earthing purposes, reducing installation costs and risks of installation errors.

Features Forbo’s unique ‘SMART’ control surface treatment making it resistant to chemical stains and scratches ensuring a durable and hygienic solution and its excellent dimensional stability ensures seams stay tight over the lifetime of the product.

Sphera EC ensures the highest hygienic properties and provides permanent ESD control.

Roll width: 2000 mm.

Thickness: 2.0 mm.

Colours: 13 colourways

Forbo’s Sphera EC collection offers designers an extensive range of contemporary colours and designs.

Matching welding rods are available in all collection colours.

Total weight (to EN ISO 23997): 2.9 kg/m².

Thermal conductivity to BS EN 12524: 0.25 W/m·K

Dimensional stability to EN ISO 23999:  ≤ 0.4 %

Sphera SD typical value: ~ 0.2 %

Electrostatics (general requirements) IEC 61340-5-1: Compliant

Electrical resistance IEC 61340-4-1(ESD STM 7.1): 1 x 104 ≤ R ≤ 106 Ω

Electrical resistance in combination with ESD control footwear IEC 61340-4-5: R ≤ 3.5 x 107 Ω

Body voltage generation,

in common with ESD control footwear IEC 61340-4-5 (ESD STM97.2): < 50 V

Sphera SD typical value: ~ 0 V <> 30 V

Electrical behaviour:  Static dissipative EN 1081:  n/a

Electrical behaviour:  Conductive EN 1081: ≤ 1 x 106 Ω

Cleanroom particle emission: ISO 14644-1: ISO 5

Consult with Forbo technical literature for details.

150 SHEETING: VINYL

Flooring roll: Homogeneous PVC to BS EN ISO 10581.

Manufacturer: Forbo Flooring Systems Ltd, High Holborn Road, Ripley, Derbyshire, DE5 3NT.  Tel: 0800 0282 162 Fax: 01772 646912.  Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk

Contact: James Morton 07887880884 email james.morton@forbo.com

Product reference: Forbo Sphera EC

BS EN ISO 10874 class: 34 very heavy/43 heavy
Width: 2000 mm.
Thickness: 2.0 mm.
Colour/ pattern: As finishes schedule

Adhesive (and primer if recommended by manufacturer):
Eurocol 640 Eurostar Special – A superior acrylic dispersion low VOC emission adhesive with a high initial grab.
Eurocol 641 Eurostar Special EL – A very low VOC emission conductive adhesive for vinyl flooring.

Seam welding: [select as required]

Hot welding with matching coloured rod.

Accessories:
Edging and cover strips, as clause 740.
Stair nosing, as clause 750.
Skirtings, as clause 770.

770 Skirting

Type: Self coved skirting

Cove former: ECF 35mm radius by Quantum Profiles tapered to architraves. Securely bond to base and background using contact adhesive. Accurately mitre at corners.

Top edge trim: UCS2 PVC capping strip by Quantum profiles.

Wall and floor should be clean, dust free and floor surface regularity to be SR1 according to BS8203:2017 (Section 6.2.3) with wall flat and a consistent 90-degree angle to floor to achieve the best installation results. Flooring and PVC profiles are fitted against the wall, floor and each other with a contact adhesive in accordance with the recommendations of the adhesive manufacturer. Such coving should be constant in radius and care should be taken to ensure that they are straight and regular to minimize the formation of voids beneath the floor covering (BS8203:2017 Section 6.12).

Securely bond to background using contact adhesive, with top edge straight and parallel with floor.

Turn flooring material up wall, securely bond to cove former and background using adhesive specified for fixing to base, and ease top of material into edge trim. Accurately mitre at corners. All joints to be hot welded in accordance with the manufacturer’s instructions.

Height: ______

Finishing: As clause 820 omitting polished finish.

Other requirements: Seek advice from Forbo for specific requirements for flooring.