To complete the clause, select the appropriate wording from below.  Highlighted text can be ‘dragged and dropped’ to save typing.

M50 RUBBER / PLASTICS / CORK / LINO / CARPET TILING / SHEETING

M50 SHEETING……….

Sarlon® 15dB. A range of heterogeneous project vinyl floor coverings with an acoustic performance of 15dB.  Its 0.7mm pure PVC wear layer provided with a PUR lacquer is outstandingly scratch and stain resistant.  Hard wearing and with an R10 slip resistance rating, its unique construction delivers exceptional residual indentation of 0.07mm for easier movement of rolling loads and indoor wheeled traffic.

Roll width:  2000mm. Thickness:  2.6mm.  Thickness of wear layer:  0.7mm

Colours:  Canyon - 23 standard colourways; Pepper – 8 standard colourways

Matching welding rods are available in all collection colours

Consult with Forbo technical literature for details.

150 SHEETING: VINYL

Fabricated underlay: 
Forbo QuickFit Subfloor System - Optional.

Flooring roll: Heterogeneous PVC to BS EN 651.
Manufacturer: Forbo Flooring UK Ltd, P O Box 1, Kirkcaldy Fife, KY1 2SB.

Tel: 0800 0282 162 Fax: 01772 646912

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk

Product reference: Forbo Sarlon 15dB
BS EN 685 class: 34 / 42
Width: 2000 mm
Thickness: 2.6 mm
Colour / pattern: [select from]

Canyon – 432208 Lime/432218 Light Green/432207 Grey Blue/432205 Yellow/432238 Grey Green/432201 Linen/432200 Ivory/432246 Orange/432228 Green/432203 Sand/432211 Light Grey/432226 Fuchsia/432217 Light Blue/432213 Beige/432209 Medium Grey/432266 Red/432227/Medium Blue/432214 Taupe/432219 Dark Grey/432247 Purple/432237 Dark Blue/432244 Chocolate/432229 Anthracite.

Pepper – 432311 Light Grey/432319 Anthracite/432312 Medium Grey/432322 Dark Grey/432337 Blue/432300 Ivory/432314 Taupe/432344 Chocolate.

Adhesive (and primer if recommended by manufacturer):
Eurocol 540 Eurosafe Special – A superior acrylic dispersion solvent-free floor covering adhesive with a high initial grab Specifiy for general purpose use.
Eurocol 640 Eurostar Special – A superior acrylic dispersion low VOC emission adhesive with a high initial grab – specify where BREEAN section HEA9 credits are required..
Eurocol 140 Euromix PU – A polyurethane resin and hardener, water-resistant 2-component PU-adhesive. – Specify where extremes of temperature or very heavy rolling loads are expected.

Seam welding: Hot welding with matching coloured rod.

Accessories:
Edging and cover strips, as clause 740.
Stair nosing, as clause 750.
Skirtings, as clause 770.

Finishing: As clause 820 omitting polish finish

Other requirements:  Seek advice from Forbo for specific requirements for flooring

770 Skirtings

Type: Self coved skirting

Cove former: 38mmradius tapered to architraves. Securely bond to base and background using contact adhesive. Accurately mitre at corners.

Top edge trim: HCS48 PVC capping strip to all other areas. Securely bond to background using contact adhesive, with top edge straight and parallel with floor.

Turn flooring material up wall, securely bond to cove former and background using adhesive specified for fixing to base, and ease top of material into edge trim. Accurately mitre at corners. All joints to be hot welded in accordance with the manufacturer’s instructions.

Height: ______

460 SMOOTHING/LEVELLING UNDERLAYMENT COMPOUND

Forbo Flooring in association with Eurocol manufacture a range of smoothing underlayment compounds. 
Forbo Eurocol 920 Europlan Alphy
Forbo Eurocol 975 Europlan Special
Forbo Eurocol 990 Europlan Direct

Forbo Eurocol 920 Europlan Alphy
A self-smoothing, tension-free hardening leveling compound for stony subfloors and especially for anhydrite subfloors and designed for leveling in layers between 0.5 and 30mm thickness.
Smooth and impervious subfloors (ceramic, granolithic, terrazzo), asphalt and bituminous floors to be primed with 044 Europrimer Multi. Highly absorbent subfloors to be primed with 044 Europrimer Multi or 049 Europrimer ABS. See clause M50/10 and 20 ‘Preparation’ for details.
Consult Forbo Flooring Ltd’s technical literature for details.

Type: Water/powder mix 
Manufacturer: Forbo Flooring UK Ltd, PO Box 1, Kirkcaldy, Fife KY1 2SB 
Tel: 0800 0282 162 Fax: 01772 646 921 
E-mail: info.flooring.uk@forbo.com Web: www.forbo-flooring.co.uk 
Product reference: Forbo Eurocol 920 Europlan Alphy
Application: Trowel or toothed smoothing trowel. Protect fresh layers against draughts and direct sunlight.
Where applying to an underfloor heated subfloor, the heating is to be turned off 24 hours before application and heat is not to be applied for at least 24 hours after application, in steps of 5°C per day.


Forbo Eurocol 975 Europlan Special
A self-smoothing leveling compound for stony subfloors and designed for leveling in layers up to 8mm thickness.
Smooth and impervious subfloors (ceramic, granolithic, terrazzo), asphalt and bituminous floors to be primed with 044 Europrimer Multi. Highly absorbent subfloors to be primed with 044 Europrimer Multi or 049 Europrimer ABS. See clause M50/10 and 20 ‘Preparation’ for details.
Consult Forbo Flooring Ltd’s technical literature for details.

Type: Water/Powder mix
Manufacturer: Forbo Flooring UK Ltd, PO Box 1, Kirkcaldy, Fife KY1 2SB 
Tel: 0800 0262 162 Fax: 01772 646 912 
E-mail: info.flooring.uk@forbo.com Web: www.forbo-flooring.co.uk 
Product reference: Forbo Eurocol 975 Europlan Special
Application: Trowel or toothed smoothing trowel applied. 
Where applying to an underfloor heated subfloor, the heating is to be turned off 24 hours before application and heat is not to be applied for at least 24 hours after application, in steps of 5°C per day.

Forbo Eurocol 990 Europlan Direct
A self-smoothing very high quality leveling compound especially suitable for critical for stony subfloors and designed for leveling in layers up to 20mm thickness.
Smooth and impervious subfloors (ceramic, granolithic, terrazzo) to be degreased with 014 Euroclean and rinsed with water. They do not normally require to be primed. Porous subfloors do not require to be primed but highly absorbent subfloors to be primed with 044 Europrimer Multi. Highly absorbent subfloors to be primed with 044 Europrimer Multi or 049 Europrimer ABS. See clause M50/10 and 20 ‘Preparation’ for details.
Consult with Forbo Flooring Ltd if applying to asphalt and bituminous floors.
Consult Forbo Flooring Ltd’s technical literature for details.

Type: Water/Powder mix
Manufacturer: Forbo Flooring UK Ltd, PO Box 1, Kirkcaldy, Fife KY1 2SB 
Tel: 01592 643777 Fax: 01592 643999 
E-mail: info@forbo-flooring.co.uk Web: www.forbo-flooring.co.uk 
Product reference: Forbo Eurocol 990 Europlan Direct
Application: Trowel or toothed smoothing trowel applied. Protect fresh layers against draughts and direct sunlight.
Where applying to an underfloor heated subfloor, the heating is to be turned off 24 hours before application and heat is not to be applied for at least 24 hours after application, in steps of 5°C per day.