To complete the clause, select the appropriate wording from below.  Highlighted text can be ‘dragged and dropped’ to save typing.

M50 RUBBER / PLASTICS / CORK / LINO / CARPET TILING / SHEETING

M50 SHEETING…………

Sarlon® 19dB. A comfortable heterogeneous vinyl floor covering combining the highest impact sound reduction of 19dB combined with class leading indentation resistance of 0.11mm max.  Extremely high wear resistance, makes it ideal for commercial applications subject to heavy traffic. The reinforced PUR treatment reduces the amount of polishing required and reduces maintenance costs. Sarlon® 19dB offers an array of combinations of colours and designs.

Roll width:  2000mm. Thickness:  Printed 3.40mm; Crystal 3.75mm.  Thickness of wear layer:  Printed 0.67mm, Cristal 0.75mm

Colour / patterns: Wood 5 Colours ; Cristal 7 colours ; Concrete 6 colours ; Uni 15 colours ; Topograhpy 1 colour ; Code Zero 13 Colours.

Matching welding rods are available in all collection colours

Consult with Forbo technical literature for details.

150 SHEETING: VINYL

Fabricated underlay: 
Forbo QuickFit Subfloor System - Optional

Flooring roll: Heterogeneous PVC to BS EN 651
Manufacturer: Forbo Flooring UK Ltd, PO Box 1, Kirkcaldy Fife, KY1 2SB.

Tel: 0800 0282 162 Fax: 01772 646912

Email: info.flooring.uk@forbo.com. Web: www.forbo-flooring.co.uk

Product reference: Forbo Sarlon® 19dB. Select from the following ranges: Wood, Cristal, Concrete, Uni, Topography, Code Zero.
BS EN 685 class: 23 / 34 / 42
Width: 2000 mm
Thickness: Printed 3.40 mm, Cristal 3.75mm

Colour / pattern: [Select from]

Wood - 438422 Carbon/438431 Natural/438423 Ecru/438420 Clay/438429 Ebony.

Cristal – 433819 Medium Grey/433811 Grey Beige/433814 Taupe/433824 Chocolate/433800 White/433801 Pearl/433899 Black.

Concrete – 433731 Natural/433720 Clay/433723 Ecru/433721 Cloud/433712 Storm/433722 Carbon. Uni – 430800 White/430899 Black/430819 Medium Grey/430805 Yellow,/430808 Lime/430801 Pearl/430826 Orange/430848 Turquoise/430811 Grey Beige/430836 Red/430817 Blue/430814 Taupe/430847 Purple/430829 Dark Grey/430824 Chocolate.

Topography – 433910 White.

Code Zero – 433219 Medium Grey/433201 Pearl/433208 Lime/433205 Yellow/433211 Grey Beige/433248 Turquoise/433226 Orange/433214 Taupe/433217 Blue/433236 Red/433224 Chocolate/433229 Dark Grey/433247 Purple.

Adhesive (and primer if recommended by manufacturer):
Eurocol 540 Eurosafe Special – A superior acrylic dispersion solvent-free floor covering adhesive with a high initial grab Specifiy for general purpose use.
Eurocol 640 Eurostar Special – A superior acrylic dispersion low VOC emission adhesive with a high initial grab – specify where BREEAN section HEA9 credits are required..
Eurocol 140 Euromix PU – A polyurethane resin and hardener, water-resistant 2-component PU-adhesive. – Specify where extremes of temperature or very heavy rolling loads are expected..

Seam welding: Hot welding with matching coloured rod.

Accessories:
Edging and cover strips, as clause 740.
Stair nosing, as clause 750.
Skirtings, as clause 770.

Finishing: As clause 820 omitting polish finish

Other requirements:  Seek advice from Forbo for specific requirements for flooring